| CML6032@IITD:~/ASSIGNMENT | VT100 ¦ Bourne shell |
| --- | --- |

20261005 CML6032 ASSIGNMENT 1 : MATERIALS CHEMISTRY, STRUCTURAL ANALYSIS

NISHEAL MICHAEL KALEY  |  ENTRY NO 2025CYS7090  |  IIT DELHI  |  10 OCTOBER 2026

VIDEO https://0nmeesheall.github.io/CML6032-Assignment1/     REPO  https://github.com/0nmeesheall/CML6032-Assignment1

NOTATION  LENGTHS IN pm (1 ANGSTROM = 100 pm), RATIOS NOT PER-100, OXIDATION STATES AS TUPLES, MIRROR PLANES AS MP, SPACE GROUPS WITH OVERHEAD BARS. THE ISSUED BRIEF IS TRANSCRIBED INTO THIS NOTATION.

SOLUTION A

| SPECIMEN | HABIT AND FORMS | MACROSCOPIC OPERATION INVENTORY | MOST PROBABLE CLASS |
| --- | --- | --- | --- |
| 1 | OCTAHEDRON {111} TRUNCATED BY CUBE {100} | 48 OPERATIONS: 3 FOUR-FOLD ALONG <100>, 4 THREE-FOLD ALONG <111>, 6 TWO-FOLD ALONG <110>, 9 MP (3 AXIAL + 6 DIAGONAL), CENTRE i, S4 AND S6 | m3̅m (Oh, CLASS 32) |
| 2 | PRISM {101̅0} PLUS BIPYRAMID {101̅1} | 24 OPERATIONS: 1 SIX-FOLD ALONG [0001] WITH COINCIDENT 3, 2, 6̅ AND S6, 6 BASAL TWO-FOLD (3 TO FACES + 3 TO EDGES), 7 MP (1 BASAL + 6 VERTICAL), CENTRE i | 6/mmm (D6h, CLASS 27) |

EXCLUSIONS	SPECIMEN 1: 432 AND 4̅3m EXCLUDED BY THE MP PLUS CENTRE; m3̅ EXCLUDED BY THE 6 FACE-DIAGONAL TWO-FOLD AXES; 23 EXCLUDED BY BOTH.

SPECIMEN 2: 6mm EXCLUDED BY THE IDENTICAL CAPS DEMANDING A BASAL MP; 6/m EXCLUDED BY THE 6 BASAL DIADS; 6 AND 622 EXCLUDED BY MP PLUS CENTRE; 6̅m2 AND THE TRIGONAL MIMICS 3̅m, 32 AND 3m EXCLUDED BECAUSE ALL 6 CAP FACES ARE EQUAL.

LIMIT	EXTERNAL FORM FIXES THE CLASS ONLY UP TO THE HOLOHEDRY OF THE LATTICE, SO THESE ARE THE MOST PROBABLE POINT GROUPS AND NOT A PROOF. PYROELECTRIC, PIEZOELECTRIC AND OPTICAL-ACTIVITY TESTS WERE NOT PERFORMED, SO CENTROSYMMETRY IS INFERRED FROM FORM EQUIVALENCE ALONE. THE SPECIMEN IDENTITIES AND THE MEASURED {100}/{111} INTERFACIAL ANGLE ISSUED IN CLASS ARE STILL TO BE ENTERED.

SOLUTION B SEGMENT 1

BASIS	Ba(+2, SPIN UNASSIGNED) 0,0,0  |  Ti(+4, SPIN UNASSIGNED) 1/2,1/2,z  |  O1(-2, SPIN UNASSIGNED) 1/2,1/2,0  |  O2(-2, SPIN UNASSIGNED) 1/2,0,1/2  |  O3(-2, SPIN UNASSIGNED) 0,1/2,1/2

MODEL	u = (z - 1/2) x LP3 ;  P = (1/V) SUM q u = 4e u / V  WITH V = 6.5325e7 pm3. NINE STATES WERE BUILT AT STEP 0.005; THE FIVE STATES NAMED IN THE BRIEF ARE THE SUBSET z = 0.480, 0.490, 0.500, 0.510, 0.520.

| z | 0.480 | 0.485 | 0.490 | 0.495 | 0.500 | 0.505 | 0.510 | 0.515 | 0.520 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ti OFFSET u / pm | -8.21 | -6.15 | -4.10 | -2.05 | 0.00 | +2.05 | +4.10 | +6.15 | +8.21 |
| Ti-O1 UP / pm | 213.3 | 211.3 | 209.2 | 207.2 | 205.1 | 203.1 | 201.0 | 199.0 | 196.9 |
| Ti-O1 DOWN / pm | 196.9 | 199.0 | 201.0 | 203.1 | 205.1 | 207.2 | 209.2 | 211.3 | 213.3 |
| P / (C m-2) | -0.0805 | -0.0604 | -0.0402 | -0.0201 | 0.0000 | +0.0201 | +0.0402 | +0.0604 | +0.0805 |
| STATE | -Ps |  | -Pr |  | Ec, P = 0 |  | +Pr |  | +Ps |

CHECKS	Ti-O1 UP PLUS Ti-O1 DOWN IS EXACTLY 410.27 pm = LP3 IN EVERY STATE; THE COLUMNS READ 410.2 OR 410.3 ONLY FROM ONE-DECIMAL ROUNDING. P(z) = -P(1 - z). THE EQUATORIAL Ti-O2 AND Ti-O3 CONTACTS MOVE ONLY FROM 199.52 pm TO 199.69 pm ACROSS THE WHOLE SCAN, SO THE DISTORTION IS ESSENTIALLY AXIAL. WORKED CASE z = 0.520: P = 4(1.602e-19)(8.21e-12) / 6.5325e-29 = +0.0805 C m-2.

HYSTERESIS	THE LOOP IS DRAWN WITH TWO BRANCHES. THE DESCENDING BRANCH REACHES P = 0 AT E = -Ec AND THE ASCENDING BRANCH REACHES P = 0 AT E = +Ec, SO IT IS DOUBLE VALUED AND NEVER PASSES THROUGH THE ORIGIN; A SINGLE S CURVE THROUGH THE ORIGIN IS NOT A HYSTERESIS LOOP. PLOTTED FROM THE MEASURED Ps = 0.26 C m-2, Pr = 0.21 C m-2 AND Ec = 0.5 MV m-1 WITH A TANH SWITCHING MODEL; IT IS A SCHEMATIC, NOT DATA.

CORRECTIONS	(1) THE Ti-ONLY RIGID-ION SUM REACHES ONLY 0.0805 C m-2 BECAUSE Ba AND O ARE HELD FIXED; THE TRUE SOFT MODE ALSO MOVES O AGAINST Ba, WHICH IS WHY THE MEASURED Ps IS 0.26 C m-2.

(2) THE POLAR PHASE OF BaTiO3 IS P4mm (No 99) BELOW Tc = 393 K AND CUBIC Pm3̅m ABOVE IT; P4/mmm IS ONLY THE NON-POLAR REFERENCE AT FIXED RATIO 1.0282 AND IS NOT AN OBSERVED PHASE.

(3) THE ISSUED RATIO 1.0282 EXCEEDS THE LITERATURE 300 K TETRAGONALITY OF ABOUT 1.011, SO THE ISSUED CELL IS AN EXAGGERATED TETRAGONAL AND THE TREND, NOT THE MAGNITUDE, IS THE RESULT.

(4) REVERSAL IS NOT HOMOGENEOUS: 180-DEGREE DOMAIN WALLS NUCLEATE AND SWEEP, WHICH IS WHY REAL Ec IS 1e5 TO 1e6 V m-1 AND NOT THE ABOUT 1e8 V m-1 A RIGID LATTICE WOULD DEMAND.

SOLUTION B SEGMENT 2

| PHASE | PROTOTYPE | SG | LP / pm | PER CELL | NEAREST / pm | CN | RADII USED / pm | SUM | DIFF | RATIO | WINDOW | VERDICT |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| NaCl | ROCK SALT | Fm3̅m | 564.0 | Na4 Cl4 | 282.0 | 6:6 | 102 + 181 IONIC | 283 | -1.0 | 0.5635 | OCTA | AGREES |
| CaTe | ROCK SALT | Fm3̅m | 635.6 | Ca4 Te4 | 317.8 | 6:6 | 100 + 221 IONIC | 321 | -3.2 | 0.4525 | OCTA | AGREES |
| CsCl | CsCl TYPE | Pm3̅m | 412.0 | Cs1 Cl1 | 356.8 | 8:8 | 174 + 181 IONIC | 355 | +1.8 | 0.9613 | CUBIC | AGREES |
| AuZn | CsCl B2 | Pm3̅m | 319.0 | Au1 Zn1 | 276.3 | 8:8 | 144 + 134 METALLIC | 278 | -1.7 | 0.9306 | NONE | METALLIC |
| CaF2 | FLUORITE | Fm3̅m | 546.3 | Ca4 F8 | 236.6 | 8:4 | 112 + 131 IONIC | 243 | -6.4 | 0.8550 | CUBIC | AGREES |
| CeO2 | FLUORITE | Fm3̅m | 541.1 | Ce4 O8 | 234.3 | 8:4 | 97 + 138 IONIC | 235 | -0.7 | 0.7029 | OCTA | FAILS, EDGE |
| K2O | ANTIFLUOR | Fm3̅m | 644.9 | K8 O4 | 279.2 | 4:8 | 137 + 142 IONIC | 279 | +0.2 | 0.9648 | CUBIC | FAILS, STOICH |
| ZnS | ZINC BLENDE | F4̅3m | 540.6 | Zn4 S4 | 234.1 | 4:4 | 122 + 105 COVALENT | 227 | +7.1 | 0.3261 | TETRA | AGREES |
| GaP | ZINC BLENDE | F4̅3m | 544.8 | Ga4 P4 | 235.9 | 4:4 | 126 + 107 COVALENT | 233 | +2.9 | 0.8492 | NONE | COVALENT |

NEAREST	UNLIKE-PAIR SEPARATION IS LP/2 FOR ROCK SALT, LP x 3^0.5 / 2 FOR THE CsCl TYPE AND LP x 3^0.5 / 4 FOR FLUORITE, ANTIFLUORITE AND ZINC BLENDE.

WINDOWS	TETRAHEDRAL 0.225 TO 0.414 (CN 4)  |  OCTAHEDRAL 0.414 TO 0.732 (CN 6)  |  CUBIC ABOVE 0.732 (CN 8). EACH WINDOW IS TWO SIDED; QUOTING ONLY ONE EDGE IS NOT A PREDICTION, AND THE RULE IS SILENT ON METALLIC AND COVALENT BONDING.

READING	CaTe IS LARGER THAN NaCl ONLY BECAUSE Te(-2) AT 221 pm EXCEEDS Cl(-1) AT 181 pm; THE TWO CATIONS DIFFER BY 2 pm, SO THE ANION SETS THE CELL. THE CsCl TYPE IS PRIMITIVE CUBIC AND NOT BODY-CENTRED, BECAUSE THE CORNER AND CENTRE CARRY DIFFERENT SPECIES. FLUORITE AND ANTIFLUORITE DIFFER ONLY BY EXCHANGING THE CATION AND ANION SITES. ZINC BLENDE FILLS HALF THE TETRAHEDRAL HOLES, WHICH REMOVES THE INVERSION CENTRE AND MAKES ZnS AND GaP PIEZOELECTRIC, UNLIKE THE CENTROSYMMETRIC ROCK SALT PAIR. CeO2 AND K2O ARE THE TWO CASES WHERE THE RADIUS-RATIO RULE FAILS AGAINST THE OBSERVED COORDINATION.

FILES	cif_prototypes/ 9 SINGLE-PHASE P1 CIFS  |  cif_batio3/ 9 STATES  |  renders/ 9 PNG  |  figures/ hysteresis_loop PNG AND PDF  |  slides/ 15-SLIDE PPTX  |  README.md. EVERY CIF IS P1 WITH THE FULL BASIS ENUMERATED, SO THE FILE MAKES NO SYMMETRY CLAIM; THE PARENT SG COLUMN IS THE IDEALISED PROTOTYPE SYMMETRY.

OUTSTANDING	THE TWO SPECIMEN IDENTITIES AS ISSUED IN CLASS AND THE MEASURED {100}/{111} INTERFACIAL ANGLE. THE WALKTHROUGH IS SERVED FROM THE REPOSITORY ITSELF AT THE VIDEO LINK ABOVE, NOT FROM YOUTUBE.

FIGURE	THE CORRECTED TWO-BRANCH HYSTERESIS LOOP IS SLIDE 08 OF THE DECK AND figures/hysteresis_loop_{dark,light}.{png,pdf} IN THE REPOSITORY.